SWIFTFORM ®
Specification Sheet

Swiftform® is a patented product that is manufactured in the UK, is used throughout the construction industry as a shuttering product. Swiftform® is made from corrugated plastic sheet and reinforced with Bright hard drawn mild steel. Wire is threaded through the flute and secured either end with a welded length of wire. This enables Swiftform® to be folded in various ways, folding with the flute and against the flute. The folding gives the product added strength. Swiftform is generally formed to produce L section side panels, U section panels - to save on blinding and specifically designed pile caps, bases and pads. It is recommended that Swiftform® laps at 50-100mm. For best use it is recommended that Swiftform is used in conjunction with gripper grade plate spacers and concrete square bar, alternatively plastic line spacers.
Corrugated Plastic
· [bookmark: _GoBack]4mm thick 700gr/m² (7mm thick for Swiftform Extra Stiff)
· 3.6mm x 3.6mm flute
· Inert, impact resistant product
· Non toxic
· Flame retardant to LPS1207 standard
· Cuts easily with a knife
Mild Steel Wire
· Bright hard drawn low carbon mild steel
· 3mm-5mm diameter
· Tensile strength 660(+/-30) N/mm²
· ISO9001/2008
· CARES accredited
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